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BURNISHED POLISHED CONCRETE
DEFINITION   -   D103.0
	The friction-rubbing of a concrete floor surface with abrasive pads until the desired level of a glossy finish is achieved.



Friction-Rubbing:  The act of changing a concrete floor surface by means of a multi step mechanical process that involves abrasive pads where each step is burnished until the desired level of glossy finish is achieved.   
· Slip Resistance: Dynamic Coefficient of Friction (DCOF) range of 0.35 to 0.45 under wet conditions when measured according to ANSI/NFSI B101.3.
· Surface Profile:  Range to be determined.

Abrasive Pads:  Diamond impregnated abrasive pads. 
Glossy Finish:  

	LEVEL
	NAME
	REFLECTIVE

CLARITY
	REFLECTIVE

SHEEN

	1
	Flat

[Ground]
	Flat appearance with no to very slight diffused reflection
	10

to

100
	None to 

very low
	15

to

80

	2
	Satin

[Honed]
	Matte appearance with or without slight diffused reflection
	
	Low to medium
	

	3
	Semi-

Polished
	Objects being reflected are not quite sharp and crisp but can be easily identified
	
	Medium to high
	

	4
	Highly-

Polished
	Objects being reflected are sharp and crisp as would be seen in a mirror-like reflection
	
	High to highest
	


· Reflective Clarity:  
-
Visual Appearance:  When viewed 5 feet above and perpendicular to a surface, the degree of sharpness and crispness of the reflection of overhead objects.  

-
Measured by Device:  Numbers indicate the Distinctness of Image on a scale of 1 (poor) to 10 (high) when measured according to ASTM D5767.
· Reflective Sheen:  
-
Visual Appearance:  When viewed at 20 feet from and at an angle to a surface, the degree of gloss reflected from a surface.  

-
Measured by Device:  Numbers indicate the Gloss at 60 degrees when measured according to ASTM D4039.
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